December 20, 2007

SPECIAL PROVISION

SP-0026(4)0 - B

# SECTION 03413S

## PRECAST SUBSTRUCTURE

### PART 1	GENERAL

#### 1.1	SECTION INCLUDES

A.	Materials and procedures for constructing, placing, and grouting precast concrete substructure elements.

#### 1.2	RELATED SECTIONS

- Section 02056: Embankment, Borrow, and Backfill

- Section 03055S: Portland Cement Concrete

- Section 03211: Reinforcing Steel and Welded Wire

- Section 03310: Structural Concrete

### PART 2	PRODUCTS

#### 2.1	CONCRETE

A.	Use Concrete Class AA(AE) per Section 03055S.

#### 2.2	REIFORCING STEEL

A.	Use reinforcing steel per Section 03211.

2.3	LIFTING INSERTS AND DEVICES

- Design type and location to be used and submit to the Engineer for approval.

2.4	PRE-QUALIFICATION

- Fabricator must be pre-qualified as a supplier of pre-cast concrete products in accordance with the “Quality Management Plan:  Precast-Prestressed Concrete Structures.”

### PART 3	EXECUTION

#### 3.1	PREPARATION

A.	Construct subgrade to the requirements of the structure plan elevations and per Section 02056.

#### 3.2	FABRICATION

A.	Do not deposit concrete in the forms until the Engineer has inspected and approved the placement of all materials in the forms per Section 03310.

#### 3.3	PLACING PRECAST CONCRETE SUBSTRUCTURE ELEMENTS

- Place to the requirements provided in the structure plan.

#### 3.3	PLACING NON-SHRINK GROUT

- Place grout in locations as shown in plans.  Place per manufacturers recommendations.

END OF SECTION