May 5, 2008

SPECIAL PROVISION

SP-0026(4)0

# SECTION 03485S

## PRECAST CONCRETE APPROACH SLAB AND DECK PANELS

### PART 1	GENERAL

#### 1.1	SECTION INCLUDES

A.	Materials and procedures for constructing, placing, and grouting precast concrete deck panels, precast concrete approach slabs and precast concrete sleeper slabs.

#### 1.2	RELATED SECTIONS

- Section 02056: Embankment, Borrow, and Backfill

- Section 03055S: Portland Cement Concrete

- Section 03211: Reinforcing Steel and Welded Wire

- Section 03310: Structural Concrete

  - REFERENCES

- ASTM C-1107

  - SUBMITTALS

- Pick Points

  - Provide shop drawings and design calculations for all panel pick points to engineer 14 days prior to construction for approval.

### PART 2	PRODUCTS

#### 2.1	CONCRETE

- Use Concrete Class AA(AE) per Section 03055S.

#### 2.2	GROUT

A.	Use a UDOT approved Non-Shrink, Non-Metallic, Non-Corrosive Grout for deck panel transverse joints, approach slab longitudinal joints, and to fill the haunch between the deck panels and girder.  Grout to conform with ASTM C-1107.

B.	Use a UDOT approved Non-Shrink, Non-Metallic, Non-Corrosive Epoxy Grout for the deck panel longitudinal joints between phases and the connection joint between end of deck and approach slab.  Grout to conform with ASTM C-1107.

#### 2.3	REIFORCING STEEL

A.	Use reinforcing steel per Section 03211.

2.4	LIFTING INSERTS AND DEVICES

- Design type and submit to the Engineer for approval.

2.5	PRE-QUALIFICATION

- Fabricator must be pre-qualified as approved by the Engineer.

### PART 3	EXECUTION

#### 3.1	PREPARATION

A.	Construct subgrade to the requirements of the structure plan elevations and per Section 02056 for approach slab and sleeper slab.

B.	Prepare girder flange for placement of the deck panels per plan details.

#### 3.2	FABRICATION

A.	Do not deposit concrete in the forms until the Engineer has inspected and approved the placement of all materials in the forms per Section 03310.

#### 3.3	PLACING PRECAST CONCRETE ELEMENTS

- Place to the requirements provided in the structure plan.

#### 3.3	PLACING NON-SHRINK GROUT

- Place grout in locations as shown in plans.  Place per manufacturers recommendations.

END OF SECTION