EPPING

13940

September 3, 2003

S P E C I A L   P R O V I S I O N

AMENDMENT TO SECTION 520 -- PORTLAND CEMENT CONCRETE

Item 520.5 – Flowable Grout Bed

This special provision provides for Flowable Grout Bed and contents of this special provision apply to this item only.  All provisions of 520 shall apply except as amended or modified below.

Add to 1.2:

1.2.4	The flowable grout bed shall meet the strength and air requirements of Class B concrete.

Add to 3.5.3

	3.5.3.9	Means to contain the flowable grout bed within a designated space shall be provided.  Approved methods to ensure completly filling the void shall be used.  The means and methods of placement shall be included in the assembly plan detailed in Section 529.

Add to 3.10.1

3.10.1.1	Curing requirements for flowable grout bed shall be waived.

Amend 4.1:

4.1	Flowable grout bed will be measured by the cubic meter (cubic yard) in place unless otherwise indicated, and in accordance with the following.

Amend 4.1.1.3:

4.1.1.3	Flowable grout bed will be measured to the form lines placed at the limits shown on the plans.  All Flowable grout bed placed where rock will not be removed shall be formed and measured in accordance with 4.1.1.2.

Amend 5.1:

5.1	The accepted quantities of flowable grout bed will be paid for at the contract unit price per cubic meter (cubic yard) complete in place, unless otherwise indicated.

Amend 5.1.1:

5.1.1	The cost of development and testing of alternate mix designs for flowable grout bed will be subsidiary to the item.

Add to Pay Item and Units:

520.5	Flowable Grout Bed	Cubic Meter (Cubic Yard)