EPPING

13940

August 25, 2003

S P E C I A L   P R O V I S I O N

AMENDMENT TO SECTION 520 -- PORTLAND CEMENT CONCRETE

Item 520.422 - Concrete Class F, Flowable Fill, Non-Excavatable (F)

This special provision provides for Class F, Flowable Fill, Non-Excavatable concrete as a final pay quantity and contents of this special provision apply to this item only.  All provisions of 520 shall apply except as amended or modified below.

Add the following to Table 1 - Classes of Concrete:

| F26 | 6.9(1000)7 | 3.0 to 4.05 | 15 to 255 |
| --- | --- | --- | --- |

6 Class F2, flowable fill, non-excavatable is a variation of class F, flowable fill.  All references made to class F, flowable fill in section 520 and amendments shall be applicable to class F2, flowable fill, non-excavatable, except as amended within this special provision.

7 Flowable fill, non-excavatable shall not have a  maximum 84 day Compressive Strength limit requirement.

Add to 3.5.3

3.5.3.9	Any significant voids created by shrinkage of the flowable fill after setting shall be filled by lean grout, soil backfill or another material acceptable to the Engineer.

Add to 3.5.5

3.5.5.6	Concrete class F, flowable fill, of any variation, shall not be deposited under water in any application.  Methods to de-water spaces to be filled by flowable fill shall be used prior to placement. The de-watering shall continue after placement until the flowable fill satisfies the setting requirement of 3.5.3.8.

Delete  4.1

Amend 4.2 to read

4.2  Concrete class F will not be measured, but shall be the cubic meter (cubic yard) final pay quantity in accordance with 109.11 for material within the limits shown on the plans.

Delete 5.1

Amend 5.2 to read

5.2  Concrete class F of the type specified will not be measured, but shall be the cubic meter (cubic yard) final pay quantity in accordance with 109.11 for material within the limits shown on the plans.

Add to Pay Item and Units:

520.422	Concrete Class F, Flowable Fill,
 Non-Excavatable (F)	Cubic Meter (Cubic Yard)