XXX

YYY

Date:

S P E C I A L   P R O V I S I O N

AMENDMENT TO SECTION 528 – PRESTRESSED CONCRETE MEMBERS

This special provision clarifies member acceptance for strength and permeability in prestressed concrete members.  All provisions of 528 shall apply except as amended or modified below.

Amend 3.1.5.2 to read:

3.1.5.2  Each member cast shall have a minimum of two additional match cured cylinders, for each thermocouple used, available for testing by the Department at 28 days (or other time interval detailed on the plans to attain design compressive strength) for quality assurance.  Acceptance of the concrete within each member will be based on successfully achieving the specified minimum average design compressive strength for two match cured quality assurance cylinders.

Amend 3.1.6.2 to read:

3.1.6.2	  Acceptance of the concrete within each bed cast will be based on successfully achieving the maximum average rapid chloride permeability value of 2500 coulombs at 56 days for two match cured quality assurance cylinders.

Add to 3.11

3.11.6	Placement of concrete in stages to facilitate box beam fabrication will be allowed.  Interval times between concrete placement stages shall be limited to 45 minutes to ensure that a cold joint has not formed between the two placement stages.  Placement plans requiring interval times longer than 45 minutes shall be approved prior to use.  Interval times extending beyond 45 minutes without prior approval is cause for rejection of the member.